【Mass Production】
Lithium bis(fluorosulfonyl)imide
双氟磺酰亚胺锂

▎ Basic Information
	Abbreviation
	LiFSI

	[bookmark: _GoBack]Product Status
	Mass Production


▎ Technical Specifications
	Test Item
	Specification

	Purity
	≥99.50 %

	Moisture
	≤100 ppm

	Free Acid
	≤100 ppm

	Chloride (Cl⁻)
	≤10.0 ppm

	Sulfate (SO₄²⁻)
	≤50 ppm



Note: The above technical specifications are typical values. Specific specifications are subject to the Certificate of Analysis (COA). For detailed product information or customized specifications, please contact our sales team.
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