【Mass Production】
Lithium bis(fluorosulfonyl)imide solution
双氟磺酰亚胺锂溶液

▎ Basic Information
	Abbreviation
	LiFSI-EMC

	Product Status
	Mass Production


▎ Technical Specifications
	Test Item
	Specification

	Mass Concentration
	（30±0.5）%

	Purity
	[bookmark: _GoBack]≥99.80 %

	Moisture
	≤20 ppm

	Free Acid
	≤50 ppm

	Chloride (Cl⁻)
	≤5.0 ppm

	Sulfate (SO₄²⁻)
	≤20 ppm



Note: The above technical specifications are typical values. Specific specifications are subject to the Certificate of Analysis (COA). For detailed product information or customized specifications, please contact our sales team.
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