【Mass Production】
Lithium bis(oxalate)borate
二草酸硼酸锂

▎ Basic Information
	Abbreviation
	LiBOB

	[bookmark: _GoBack]Product Status
	Mass Production


▎ Technical Specifications
	Test Item
	Specification

	Purity
	≥99.50 %

	Moisture
	≤300 ppm

	Free Acid
	≤130 ppm

	Chloride (Cl⁻)
	≤5.0 ppm

	Sulfate (SO₄²⁻)
	≤50 ppm



Note: The above technical specifications are typical values. Specific specifications are subject to the Certificate of Analysis (COA). For detailed product information or customized specifications, please contact our sales team.
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