【Mass Production】
Lithium difluorobis(oxalate)phosphate solution
二氟二草酸磷酸锂溶液

▎ Basic Information
	Abbreviation
	LiDFOP

	Product Status
	Mass Production


▎ Technical Specifications
	Test Item
	Specification

	Mass Concentration
	（20.0±2.0） %

	Moisture
	[bookmark: _GoBack]≤50 ppm

	Free Acid
	≤200 ppm

	Chloride (Cl⁻)
	≤5.0 ppm

	Sulfate (SO₄²⁻)
	≤10.0 ppm



Note: The above technical specifications are typical values. Specific specifications are subject to the Certificate of Analysis (COA). For detailed product information or customized specifications, please contact our sales team.
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