【Pilot Scale】
Tetrahydrofuro[3,4-d][1.3.2]dioxathiole 2.2-dioxide
赤藓糖双环硫酸酯

▎ Basic Information
	Abbreviation
	THFDTD

	[bookmark: _GoBack]Product Status
	Pilot Scale


▎ Technical Specifications
	Test Item
	Specification

	Purity
	≥99.5 %

	Moisture
	≤50 ppm

	Free Acid
	≤50 ppm

	Chloride (Cl⁻)
	≤20 ppm

	Sulfate (SO₄²⁻)
	≤50ppm



Note: The above technical specifications are typical values. Specific specifications are subject to the Certificate of Analysis (COA). For detailed product information or customized specifications, please contact our sales team.
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