【Mass Production】
Prop-1-ene-1,3-sultone
丙烯基-1,3-磺酸内酯

▎ Basic Information
	Abbreviation
	PST/PRS

	[bookmark: _GoBack]Product Status
	Mass Production


▎ Technical Specifications
	Test Item
	Specification

	Purity
	≥99.8 %

	Moisture
	≤50 ppm

	Free Acid
	≤50 ppm

	Chloride (Cl⁻)
	≤5.0 ppm

	Sulfate (SO₄²⁻)
	≤10.0 ppm



Note: The above technical specifications are typical values. Specific specifications are subject to the Certificate of Analysis (COA). For detailed product information or customized specifications, please contact our sales team.
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