【Mass Production】
Lithium methylsulfate
甲基硫酸锂

▎ Basic Information
	Abbreviation
	LMS

	[bookmark: _GoBack]Product Status
	Mass Production


▎ Technical Specifications
	Test Item
	Specification

	Purity
	≥99.0 %

	Moisture
	≤100 ppm

	Free Acid
	≤100 ppm

	Chloride (Cl⁻)
	≤10 ppm

	Sulfate (SO₄²⁻)
	≤800 ppm



Note: The above technical specifications are typical values. Specific specifications are subject to the Certificate of Analysis (COA). For detailed product information or customized specifications, please contact our sales team.
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