【Pilot Scale】
2-Fluoro-1,3,2-dioxaphospholane
2-氟-1,3,2-二氧磷杂环戊烷

▎ Basic Information
	Abbreviation
	FDOPP

	[bookmark: _GoBack]Product Status
	Pilot Scale


▎ Technical Specifications
	Test Item
	Specification

	Purity
	≥98.5%

	Moisture
	≤100 ppm

	Free Acid
	≤100 ppm

	Chloride (Cl⁻)
	≤5 ppm

	Sulfate (SO₄²⁻)
	≤10 ppm



Note: The above technical specifications are typical values. Specific specifications are subject to the Certificate of Analysis (COA). For detailed product information or customized specifications, please contact our sales team.
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